IO1686T

Tri-Layer One Way Vision

Description：

Film：     180 micron; black & white PVC film

Adhesive： Clear removable adhesive

Liner：    100gsm perforated double PE liner and 100gsm raw paper

Width：   0.98/1.07/1.27/1.37/1.52m

Features：

- Excellent printability and handling, superior appearance;

- One side visual, opque and privacy protection; Hole size 1.40mm, perforation 30%;

- Thickening of PVC film, good stiffness, easy application, anti – tear during construction ;

- Good dimensional stability after application and outdoor durability and performance.

Applications：

- Applicable to glass surface, also applicable to transparent acrylic, PVC, PET transparent panels;

- Suitable for various of solvent ink, Eco-solvent HP Latex & UV ink.

Technical Data：

Testing condition: Indoor temperature 23±2°C; Relative humidity 50±5%;

Use aluminum, glass, steel plate as the base material for testing.

| Test Items | units | Test method | Average value |
| --- | --- | --- | --- |
| Thickness PVC Weight-Liner Weight -finished product Initial adhesive Dimensional stability MD Dimensional stability CD Tensile strength MD Tensile strength CD Construction temperature Applicable temperature | Micron g/m² g/m² N/25mm mm mm N/25 mm N/25 mm ℃ ℃ | GB/T6672-2001 GB4669-1995 GB4669-1995 FTM 9 FTM 14 FTM 14 GB/T1040.1-2006 GB/T1040.1-2006 | 180±10 180±10 380±20 ≥4 ≤0.6 ≤0.5 ≥40 ≥35 20±10℃ -20～+70 |

- All technical data is subject to change without prior notice

Storage Condition：

All INFLEX products need to be stored in the original packing and with the original protection materials, preferably stored hermetically, no more than 6 layers if stored horizontally. Do not expose in direct sunlight or heat sources.

Production and Application Environment：

Production environment: temperature of 25 ± 5 °C, relative humidity of 50%±10%, clean dust-free environment without suspended matter; Please move the materials to the printing environment 24 hours before printing. Printing test before use and remain enough edge margins when printing.

Application Environment：

Temperature of 25 ± 5 °C, relative humidity of 50%±10%, paste on clean ,smooth, even, dust-free substrate surface.

Warranty Condition：

One year shelf life: stored in suitable conditions, preferably use within 6 months;

Two year prosecution period: from the product manufacture date, no-acceptance for overdue product.

Important Remark：

The information mentioned in this product data sheet is based upon tests that were executed by INFLEX, and that we consider to be reliable. Environment humidity more than 70% in different district will decrease the printing result.

Product Application：