ND1000G

Black Cutting Sticker

Description：

Film: 80micron black glossy PVC film；

Adhesive: Transparent permanent adhesive；

Liner: 120 gsm white PEK paper with one side PE & Silicon coating

Width: 1.06/1.22/1.27/1.37/1.52m

Features：

- With colorful and personalized decoration, strong covering power.

- PVC film, dirt proof, water proof, one year outdoor weather resistance .

Applications：

- Suitable for vehicle body decoration, cutting, DIY, indoor and outdoor decoration and other fields.

- Not for printing, while digital engraving into the needed pattern, with transferable film the pattern will be transferred onto the printed items.

Technical Data：

Testing condition: Indoor temperature 23±2℃, Relative humidity 50±5%.

| Test Items | Unit | Test Method | Average value |
| --- | --- | --- | --- |
| Thickness PVC Weight-Liner Weight-finished product Gloss Rate 60° Initial Adhesion 24h, 180°peel Dimensional stability MD Dimensional stability CD Tensile strength MD Tensile strength CD Construction Temperature Applicable Temperature | Micron g/m² g/m² % N/25mm N/25mm mm mm N/25 mm N/25 mm ℃ ℃ | GB/T6672-2001 GB4669-1995 GB4669-1995 GB8807-88 FTM 9 FTM 1 FTM 14 FTM 14 GB/T1040.1-2006 GB/T1040.1-2006 | 80±10 120±10 250±20 ≥20 ≥8 ≥10 ≤1.8 ≤1.5 ≥30 ≥20 20±10℃ -20～+70 |

- All technical data is subject to change without prior notice.

Storage Condition：

All NAR products need to be stored in the original packing and with the original protection materials, preferably stored hermetically and vertically, do not expose to direct sunlight or heat sources. In order to avoid loss of quality, NAR products should also be stored in suitable conditions, that is at a temperature of 25°C ± 5°C and a relative humidity of 50 ± 15%. Under these conditions, NAR products can be stored up to one year.

Production and Application Environment：

Production environment: temperature of 25 ± 5 °C, relative humidity of 50%±10%, clean dust-free environment without suspended matter; Please move the materials to the printing environment 24 hours before printing. Printing test before use, Printing ink temperature of 18°C -28 °C, Equipment preheating temperature of 30 °C.

Application environment: temperature of 18 °C to 28 °C, relative humidity of 50±15%.

Warranty Condition ：

- One year service life: stored in suitable conditions, preferably use within six months.

- One year prosecution period: from the product manufacture date, no-acceptance for overdue product.

Important Remark：

The information mentioned in this product data sheet is based upon tests that were executed by NAR, and that we consider to be reliable. Advise to use the same batch. Please evaluate on the project environment in advance to confirm the products suitability.